## Slide 1: FinFET-7nm-Mock-PDK Abstraction

## Slide 2
A 7nm- Mock PDK Based on Following Reference:
[1] L. Clark et al., "ASAP7: A 7-nm finFET predictive process design kit," Elsevier Microelectronics Journal, vol. 53, pp. 105-115, 2016.
Notes: 2
2

## Slide 3
Introduction: BEOL Stack in MOCK Process
9_3MA_2MB_2MC_2MD
Total number of layers
Group A/B/C/D layers
M1-M3; M4-M5; M6-M7;M8-M9
Source: Table 1 of Ref. [1]
***Selection of Number of layers in each group is based on Table1 of Ref. [1]
***The pitch values for each group of metal layers may vary
Notes: 3
3

## Slide 4
Definition of Design Rules:
Layer: Defines the name of a layer e.g. Poly, M1 etc.
LayerNo: This number is used for layer mapping in GDSII generation
Type: A layer can be ‘Signal’ or ‘Power’ or ‘Via’ type; Depending on its type the layer can be used for ‘Signal’ or ‘Power’ routing or for a connection b/w two layers i.e., ‘Via’
Direction: Defines the allowed direction for a layer e.g. V (Vertical) or H (Horizontal); for ‘Via’ layer direction is not applicable (NA)
Width: Defines width of a layer; for all the layers (except Type == Power) width is fixed, however, for ‘Power’ layer ‘Width’ signifies the minimum allowed width and can have a larger value
Pitch: Center-to-Center distance for the same layer (Fig. 1); for ‘Via’ layer pitch is not applicable
End-to-End: Minimum end-to-end spacing for the same layer (Fig. 2); NA for ‘Via’ layer
Pitch
End-to-End
Fig. 2
Fig. 1
Notes: 4
4
4

## Slide 5
Definition of Design Rules:
MinL: Minimum length of a layer; Please note that length is along a layer ‘Direction’
MaxL: Maximum allowed length for a layer
Space: Minimum spacing between same ‘Via’ layer (Fig. 3); This rule is only applicable to ‘Via’ layer
Venc: Minimum enclosure of a Via by a Metal layer along its ‘Direction’ (Fig. 4)
Fig. 3
Space
Space
Fig. 4
Venc
Direction = H
Venc
Direction = V
Via
Notes: 5
5
5

## Slide 6
Layer | Pitch/Space* | Width | Direction | Comment/Ref.
Poly | 54 | 20 | V | Ref. for pitch and width: Table1 of [1]
Fin | 27 | 7 | H | Ref. for pitch and width: Table1 of [1]
M1 | 54 | 18 | V | Ref. for width: Table1 of [1]; we have abstracted the pitch, in [1] pitch is 36nm
M2 | 54 | 18 | H | Ref. for width: Table1 of [1]; we have abstracted the pitch, in [1] pitch is 36nm
M3 | 54 | 18 | V | Ref. for width: Table1 of [1]; we have abstracted the pitch, in [1] pitch is 36nm
V0 | 25* | 18 | NA | Ref. for width/space: Table1 of [1]
V1-V2 | 25* | 18 | NA | Ref. for width/space: Table1 of [1]
V1-V2_enclosure | NA | 7 | NA | V1-V2 enclosure by M1-M3: we have selected the value (~40% of Via width)
FinFET Mock PDK Abstraction

## Slide 7
Layer | Pitch/Space* | Width | Direction | Comment/Ref.
M4 | 72 | 24 | H | Ref. for width: Table1 of [1]; we have abstracted the pitch, in [1] pitch is 48nm
V3 | 25* | 18 | NA | Ref. for width/space: Table1 of [1]
V3_enclosure | NA | 7 | NA | V3 enclosure by M3-M4: we have selected the value (~40% of Via width)
M5 | 72 | 24 | V | Ref. for width: Table1 of [1]; we have abstracted the pitch, in [1] pitch is 48nm
V4-V5 | 34* | 24 | NA | Ref. for width/space: Table1 of [1]
V4-V5_enclosure | NA | 10 | NA | V4-V5 enclosure by M4-M6: we have selected the value (~40% of Via width)
M6 | 96 | 32 | H | Ref. for width: Table1 of [1]; we have abstracted the pitch, in [1] pitch is 64nm

## Slide 8
Layer | Pitch/Space* | Width | Direction | Comment/Ref.
M7 | 96 | 32 | V | Ref. for width: Table1 of [1]; we have abstracted the pitch, in [1] pitch is 64nm
V6-V7 | 45* | 32 | NA | Ref. for width/space: Table1 of [1]
V6-V7_enclosure | NA | 13 | NA | V6-V7 enclosure by M6-M8: we have selected the value (~40% of Via width)
M8 | 96 | >=40 | H | Ref. for width: Table1 of [1]; we have abstracted the pitch, in [1] pitch is 80nm
M9 | 96 | >=40 | V | Ref. for width: Table1 of [1]; we have abstracted the pitch, in [1] pitch is 80nm
V8 | 57* | 40 | NA | Ref. for width/space: Table1 of [1]
V8_enclosure | NA | 16 | NA | V8 enclosure by M8-M9: we have selected the value (~40% of Via width)

## Slide 9
Layer | Pitch/Space* | Width | Direction | Comment/Ref.
SDT/LISD | 54 | 24 | V | Ref. for pitch and width: Table1 of [1]
LIG | 54 | 18 | H | Ref. for pitch: Table1 of [1]; we have abstracted the width
Active | 92* | >=16 | NA | Ref. for Horizontal width and spacing: Table1 of [1]
Active.1 | NA | >=27 | NA | Ref. for Vertical width: sub-section 4.2 of [1]
GCUT | NA | 18 | NA | We have selected the value
LIG to LISD | 14* | NA | V | Distance b/w LIG to LISD end-points: Table2 of [1]
LIG/LISD/M1-M3 end-to-end | 31* | NA | NA | Table2 of [1]
Active/N-P Select to Well | 27* | NA | V | Ref. for Vertical width: sub-section 4.2 of [1]
***Fig. 1, 4-7 of [1] are also used to select some of the values |  |  |  |